NBS SPECIFICATION CARPET TILES

Valid from 01/02/2016

Version n° M02/16

**39**

**Opposite**

M50 RUBBER/PLASTICS/CORK/LINO/CARPET/SHEETING

130 CARPET TILE **modulyss® Opposite**

**Manufacturer**

Name: modulyss®

Web: [www.modulyss.com](http://www.modulyss.com)

Tel: 0800 09 62 702

**PRODUCT DESCRIPTION**

Minituft® loop pile carpet tile, 100% PA 6 Solution Dyed, Back2Back backing

**INSTALLATION METHOD**

Checkerboard on low VOC tackifier adhesive

**Number of colours**

Available in 11 colourways

**Technical specifications**

Construction Minituft®

Pile gauge 5/64”

Pile material 100% PA 6 Solution Dyed

Total weight Ca. 4400 g/m²

Pile weight Ca. 500 g/m²

Pile height Ca. 1,0 mm

Total height Ca. 5,8 mm

Pile density Ca. 0,160 g/cm³

Tuft density Ca. 200.000 /m²

Dimensions 500 x 500 mm

Dimensional stability (EN 986) max. 0,2%

Wear classification (EN 1307) 33- LC1

Fire (EN 13501-1) Cfl-s1

Warranty 15 year wear warranty and 15 year anti-static warranty.
Full details available on request.

**COLOUR**

Insert 3 digit colour ref

All technical specifications <http://www.modulyss.com/en_gb/collections/Opposite/>