NBS SPECIFICATION CARPET TILES

Valid from 01/02/2016

Version n° M01/14

**15**

**perpetual**

M50 RUBBER/PLASTICS/CORK/LINO/CARPET/SHEETING

130 CARPET TILE **modulyss® Perpetual**

**Manufacturer**

Name: modulyss®

Web: [www.modulyss.com](http://www.modulyss.com)

Tel: 0800 09 62 702

**PRODUCT DESCRIPTION**

Tufted loop pile carpet tile, 100% Polyamide, Back2Back backing

**INSTALLATION METHOD**

Monolithic, Checkerboard, Ashlar, Brick on low VOC tackifier adhesive

**Number of colours**

Available in 33 colourways, Special colours possible

**Technical specifications**

Construction Tufted

Pile gauge 1/10”

Pile material 100% Polyamide

Total weight Ca. 4600 g/m²

Pile weight Ca. 700 g/m²

Pile height Ca. 3,5 mm

Total height Ca. 6,9 mm

Pile density Ca. 0,128 g/cm³

Tuft density Ca. 104.000 /m²

Dimensions 500 x 500 mm

Dimensional stability (EN 986) max. 0,20%

Wear classification (EN 1307) 33- LC2

Fire (EN 13501-1) Bfl-s1

Warranty 15 year wear warranty and 15 year anti-static warranty.
Full details available on request.

**COLOUR**

Insert 3 digit colour ref

All technical specifications <http://www.modulyss.com/en_gb/collections/Perpetual/>